Table 1: Fatty acid composition of Jatropha oil

| Fatty acid | Composition (wt %) |
| --- | --- |
| Oleic (C18:1) | 44.9 |
| Linoleic (C18:2) | 34.1 |
| Palmitic (C16:0) | 12.2 |
| Stearic (C18:0) | 7.33 |
| Linolenic (C18:3) | 0.17 |

Table 2: Chemical composition of different NiMo/AC catalysts

| Catalysts | Nominal (wt.%) |  |  | Chemical analysis (wt.%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ni | Mo | Ni:Mo | Ni | Mo | Ni:Mo |
| Commercial | 4.2b | 10.9b | 0.38 | - | - | - |
| Ni3Mo10/AC | 3 | 10 | 0.30 | 4.5 | 12.4 | 0.36 |
| Ni3Mo15/AC | 3 | 15 | 0.20 | 4.4 | 17.4 | 0.25 |
| Ni5Mo10/AC | 5 | 10 | 0.50 | 6.9 | 12.0 | 0.57 |
| Ni5Mo15/AC | 5 | 15 | 0.33 | 6.1 | 16.0 | 0.38 |

aOn dry ash free basis   bObtained by x-ray fluorescence

Figure 1: SEM micrographs of variable concentration of NiMo/AC catalysts

Figure 2: FT-IR spectra of Jatropha oil and products.

Figure 3: Selectivity of catalysts toward various fractions of hydrocarbons obtained in the HDO process of Jatropha oil.

Figure 4: Composition of the gaseous products after HDO of Jatropha oil for the different catalysts (H2 balance)

Figure 5: Effect of Ni and Mo concentration (wt. %) in the selectivity toward C17 and C18 hydrocarbons